## Slide 1: Journal Club Articles from 2013.04.20. to 2013.04.27.
Topological Insulator Materials - Yoichi Ando http://xxx.lanl.gov/abs/1304.5693
Diamond shows promise for a quantum Internet - Richard Van Noorden http://www.nature.com/news/diamond-shows-promise-for-a-quantum-internet-1.12870
Competition between the Superconducting Proximity Effect and Coulomb Interactions in a Graphene Andreev Interferometer - Fabio Deon, Sandra Šopić, Alberto F. Morpurgo http://xxx.lanl.gov/abs/1304.6578
A ballistic pn junction in suspended graphene with split bottom gates - Anya L. Grushina, Dong-Keun Ki, Alberto F. Morpurgo http://xxx.lanl.gov/abs/1304.6844
Nanoseminar 2013.05.02.

## Slide 2
A ballistic pn junction in suspended graphene with split bottom gates
Anya L. Grushina, Dong-Keun Ki, Alberto F. Morpurgo
Department de Physique de la Matiere Condensee (DPMC) and Group of Applied
Physics (GAP), University of Geneva, 24 Quai Ernest-Ansermet, CH1205 Geneve,
Switzerland
http://xxx.lanl.gov/abs/1304.6844
Nanosemiar 2013.05.03. - Márton Attila

## Slide 3
A ballistic pn junction in suspended graphene with split bottom gates
Sample preparation
Nanoseminar 2013.05.02.
doped Si substrate covered with 300 nm SiO2
predefined gate electrodes (10 nm Ti/30 nm Au)
450-nm-thick LOR layer (polydimethylglutarimide (PMGI)-based lift-of resist)
Ti/Au electrodes (10/60 nm)
single layer graphene
water soluble polymer a 9 wt.% poly(4-styrenesulfonic acid) solution in water)
PMMA
1,6 um

## Slide 4
A ballistic pn junction in suspended graphene with split bottom gates
Sample preparation - Setup
Nanoseminar 2013.05.02.
doped Si substrate covered with 300 nm SiO2
predefined gate electrodes (10 nm Ti/30 nm Au)
450-nm-thick LOR layer (polydimethylglutarimide (PMGI)-based lift-of resist)
Ti/Au electrodes (10/60 nm)
single layer graphene
water soluble polymer a 9 wt.% poly(4-styrenesulfonic acid) solution in water)
PMMA
1,6 um
V2
V1
high current annealing @ 4.2K
transport measurements as a function of V1 and V2 @ 250 mK
electrical tuning of the charge carrier density
P-N junction

## Slide 5
A ballistic pn junction in suspended graphene with split bottom gates
Nanoseminar 2013.05.02.
V2
V1
n1 [1010 cm-2] = 1.0xV1 [V] + 0.35 xV2 [V] + 0.5
n2 [1010 cm-2] = 0.2 xV1[V] + 1.4x V2 [V] – 0.4
1,6 um

## Slide 6
A ballistic pn junction in suspended graphene with split bottom gates
Nanoseminar 2013.05.02.
V2
V1
opposite polarity regions results p-n junction
1,6 um

## Slide 7
A ballistic pn junction in suspended graphene with split bottom gates
Nanoseminar 2013.05.02.
V2
V1
opposite polarity regions results p-n junction
large contribution to the resistance
Fabry-Perot oscillations
(previously in graphene p-n-p junctions on Si/SiO2 substrate)
1,6 um

## Slide 8
A ballistic pn junction in suspended graphene with split bottom gates
Nanoseminar 2013.05.02.
V2
V1
Fabry-Perot oscillations
(previously in graphene p-n-p junctions on Si/SiO2 substrate)
two F-P vcavities (between M-G , GP-GN and G-M interface)
 checkboard pattern
From ∆n the size of the cavities can be extracted  ~ 800um
(a simple particle-in-a-box approximation)
1,6 um

## Slide 9
A ballistic pn junction in suspended graphene with split bottom gates
Nanoseminar 2013.05.02.
Applying B magnetic field – further evidence for F-P oscillations

## Slide 10
A ballistic pn junction in suspended graphene with split bottom gates
Nanoseminar 2013.05.02.
Applying B magnetic field – further evidence for F-P oscillations
exhibits a phase shift at B ~20-30 mT (<<250-300mT)
the perpendicular B field bend the electron trajectories in the cavities
critical B field when in p-space the origin is included  additional Berry- phase (π) is acquired

## Slide 11
A ballistic pn junction in suspended graphene with split bottom gates
Nanoseminar 2013.05.02.
Applying B magnetic field – further evidence for F-P oscillations
exhibits a phase shift at B ~20-30 mT (<<250-300mT)
the perpendicular B field bend the electron trajectories in the cavities
critical B field when in p-space the origin is included  additional Berry- phase (π) is acquired
temperature-dependaence of the oscillations
  - oscillations vanished @ 40K ~3,5meV

## Slide 12
A ballistic pn junction in suspended graphene with split bottom gates Anya L. Grushina, Dong-Keun Ki, Alberto F. Morpurgo
Department de Physique de la Matiere Condensee (DPMC) and Group of Applied
Physics (GAP), University of Geneva, 24 Quai Ernest-Ansermet, CH1205 Geneve,
Switzerland
http://xxx.lanl.gov/abs/1304.6844
1,6 um
Presence of p-n juntcion
Ballistic regime comparable to the device size
Preparation process preserves the high quality of the material