## Slide 1
Electrical control over single hole spins in nanowire quantum dots
Gergő
NanoJC
22/02/2013
V. S. Pribiag, S. Nadj-Perge, S. M. Frolov, J. W. G. van den Berg, I. van Weperen, S. R. Plissard, E. P. A. M. Bakkers and L. P. Kouwenhoven
arXiv:1302.2648

## Slide 2: Outline
Holes in III-V semiconductors
  strong spin-orbit interaction
  different effective mass
  weak coupling to nuclear spins → longer coherence times
    holes with p-orbitals: contact hyperfine interaction vanishes
    (10.1103/PhysRevB.78.155329)
Hole quantum dots
  fabrication is challenging
  conventional p-doped quantum wells: low stability and tuneability
  InSb nanowire: high stability&tuneability → direct comparison of electrons and holes

## Slide 3: Basic device
InSb nanowire
  precise control over crystal structure
  small bandgap (≈0.2 eV)
  100 nm in diameter, 2-3 μm long
Basic device
  demonstration of ambipolar transport
  285 nm SiO2, Ti/Au contacts, 300 nm spacing
  300 mK base temperature

## Slide 4: Defining quantum dots
Device with finger gates
  Ti/Al contacts
  InSb nanowire
  25 nm Si3N4
  finger gates (gate widths&inter-gate spacing ≈30 nm)
  50 nm Si3N4
  wide gate

## Slide 5: Defining quantum dots
Confining potential
  Single dot:
  negative voltage on a single gate
  npn-like NW
  Double dot
  using gates 2&3 → strong interdot coupling using gates 2&4 → weak interdot coupling
  nppn-like NW

## Slide 6: Measurements on the basic device
Determination of the bandgap
  large bias stability diagram of the basic device
  bandgap ≈ 0.2 eV

## Slide 7: Single dot measurements
Stability diagram
  few hole regime
  direct tunneling in the conduction band over Vsd≈90 mV

## Slide 8: Single dot measurements
Stability diagram
  resonances ending at the 0h diamond?
  g-factor≈35 → electrons → DOS of the n-type leads

## Slide 9: Double dot measurements
Few-hole double dot

## Slide 10: Double dot measurements
g-factor measurements
  Pauli spin blockade
  lifted by EDSR
  cross section at f=3.4 GHz
  2-axis vector magnet → investigation of anisotropy

## Slide 11: Double dot measurements
g-factor measurements
  electron g-factor ≈35-45
  hole g-factor ≈0.5-4
  → gate-induced g-tensor modulation also contributes to the EDSR mechanism (apart from the direct SOI)

## Slide 12: Double dot measurements
g-factor measurements
  peak at B=0 due to hyperfine interaction → Ae/Ah≈7

## Slide 13: Double dot measurements
strong interdot coupling regime
  spin blockade lifted by finite B → dip at B=0
  for electrons: mixing of states by SOI → anisotropic
  for holes, it's isotropic!

## Slide 14: The end
  Thank you for your attention!