## Slide 1: A few things you’ve (n)ever wanted to know about Graphene Nanoribbons (GNRs)
Tóvári Endre, nanoszeminárium ea., 2013. máj.31.

## Slide 2
Motivation: graphene nanoribbons
A lot of methods, with different degrees of details
Overview of basic transport properties
Y.-W. Son, M. L. Cohen, S. G. Louie, Nature Letters, Vol. 444, 16 November 2006

## Slide 3
NANO LETTERS, 2009, Vol. 9, No. 7, 2600-2604

## Slide 4
Nature 466, 470–473 (22 July 2010)
Molecular model
DFT-sim.
STM
on Au(111) single crystal

## Slide 5
Fluorine-assisted Reactive Ion Etching of SiC
Step flow and relaxation at 1300°C
Self-organized GNR formation
Gate dielectric (39nm thick) and top gate fabrication
2 µm
Nature Nanotechnology 5, 727–731 (2010)

## Slide 6
GNRs on SiC
Nature Nanotechnology 5, 727–731 (2010)
VD=-4V
2-terminal, top gate length 450 nm
Room temp.
Probably a few layers
Mobility 900-2700 cm2/Vs
40 nm
4K
RT
2-terminal, top gated
„representative ribbons”
Notes: SiO2: dn/dVg≈0,07*1012 cm-2/V

## Slide 7
Nano Res (2010) 3: 110–116
Carbothermal etching
700°C in Ar
SiO2+C
35 nm

## Slide 8
C A R B ON 5 6 ( 2 0 1 3 ) 3 3 2 –3 3 8
Selective etching of armchair edges in graphite
annealing HOPG in an oxygen containing (<45%) atmosphere: 600°C, 5-20 min
G. Dobrik *, L. Tapaszto´ , L.P. Biro

## Slide 9
C A R B ON 5 6 ( 2 0 1 3 ) 3 3 2 –3 3 8
Selective etching of armchair edges in graphite

## Slide 10
MEMS heater used for ultrastable in situ heating of graphene inside the TEM, used for self-repair of graphene defects
STEM imaging of graphene is achieved by fast scanning
is achieved by scanning 1000 times slower by using a longer dwell time
Orientation selective

## Slide 11
Appl. Phys. Lett. 101, 213101 (2012)
AFM-cutting

## Slide 12
AFM-tip assisted electrochemical etching
Small. 2010 Jul 19;6(14):1469
2,5K
0,002-0,2 e2/h
Solid State Communications 147 (2008) 366

## Slide 13
Water dissociation due to DC voltage, polarity-dependent reaction to graphene (H or O)

## Slide 14
Nature Nanotechn. 3, 397 (2008)

## Slide 15
Electron-beam lithography and plasma etching
Appl. Phys. Lett. 91, 192107 2007
protective mask
36 nm wide, 500 nm long
PRL 104, 056801 (2010)
Reproducible cond.peaks in the gap region
arXiv:0909.3886v2
10 µS≈0,129 e2/h
85 nm x 500 nm
Molitor, …, Enslin, PRB 79, 075426, 2009
Han: µh~160, µe~570
Enslin: side gated! No corr., µh~1490
Avouris Physica E 40 (2007) 228 (nem az a PRB-s cikk a kapacitásról): 200 nm oxid, 100nmx1000nm,4K, µ~530
Arxiv 0909.3886v2:
300 nm oxid, 30x200nm, µh~42
PRL 98, 206805 (Han):log scales, 1,7K
24 nm x 2 um: hole mob.110,
49 nm x 2 um: 215
71 nm: 875 cm2/Vs
Adv. Mater. 2011, 23, 3061–3065:
L=500 nm, RT
Estimated mobilities (log scale!)
W= 6 nm: µh~18 cm^2/Vs
W=10 nm: µh~41
22 nm: 51
45 nm: 300
80 nm: 640
1000 nm: 3290
Graphene edge lithography:
RT, 10 nm x 700 nm: mob.26 (VSD=1V)
RT, 20 nm, 700 nm(?): 9 (maybe already top-gated, ireelevant model
Mobilities estimated by me based on PRB 78, 161409
Avouris PRB 78, 161409
30 nm x 850 nm: 200 mob. (80K)
30x900 nm: 165 (90K)
30x1700 nm: 130 (33K)
Han: µh~160, µe~570
Enslin: side gated! No corr., µh~1490

## Slide 16
Electron-beam lithography and plasma etching
arXiv:0909.3886v2
Suggestion:
Confinement gap
Disorder potential: edge roughness+potential inhomogeneities (charged impurities in the substrate)”puddles” and tunnel barriers
Multiple quantum dots in series/parallel
Why?
The transport gap is given by the confinement+disorder amplitude
QDs in series: overlapping Coulomb-diamonds in the stability diagram

## Slide 17
Electron-beam lithography and plasma etching
arXiv:0909.3886v2
Annealing (Ar, 300°C) shrinks the transport gap, the SD-gap changes arbitrarily (rearrangement)
No correlation between the 2 gap values
Length:
W=30 nm
PRL 104, 056801 (2010)
Distance from Vg=0 increases with the value of the transport gap ΔVg
ΔVg it’s a measure of sample doping by charged impurities of the substrate; really determinded by the disorder potential

## Slide 18
Electron-beam lithography and plasma etching
arXiv:0909.3886v2
The transport gap has little length dependence, unlike the SD-gap:
Only qualitative trend, but supports the picture: a longer ribbon has more QDs whose energies need to be appropriately positioned

## Slide 19
Electron-beam lithography and plasma etching
arXiv:0909.3886v2
Short ribbons: might be smaller then the average puddle of localized carriers (~20nm), no transport and SD-gap,
Fabry-Pérot-like oscillations (like CNTs)
A few things of interest
Constant peak spacing (within the transport gap) in a 200 nm-long (!) and 30 nm wide ribbon
(in a certain region of backgate voltage):
Single QD-like behaviour
µh~42 cm2/Vs

## Slide 20
Electron-beam lithography and plasma etching
arXiv:0909.3886v2
A few things of interest
From peak spacing (0,05V) and ribbon geometries 100 nm long QD in the 200 nm x 30 nm ribbon

## Slide 21
500 nm
900 nm x 30 nm
arXiv:0909.3886v2
Fabrication method with e-beam lithography and plasma etching:
Usual resist etch mask + Ti etch mask (30 nm wide line), later removed by HCl
Additional lithography step:
Bulk mobility 6000 cm2/Vs 800 cm2/Vs
Electron-beam lithography and plasma etching

## Slide 22
Electron-beam lithography and plasma etching
PRL 104, 056801 (2010)
About width dependence
arXiv:0909.3886v2
(?)

## Slide 23
Electron-beam lithography and plasma etching
PRL 104, 056801 (2010)
T>T*:
thermally activated transport
Ea=285K
T<T*: variable range hopping, γ=1/2

## Slide 24
Electron-beam lithography and plasma etching
PRL 104, 056801 (2010)

## Slide 25
65 nm x 100 nm
Molitor, …, Enslin, PRB 79, 075426, 2009
See also: PRL 108, 266601 (2012)

## Slide 26
H-plasma etching
Adv. Mater. 2010, 22, 4014–4019
etching at ~500°C
edges parallel with the zigzag direction
TEM:
edge roughness<1nm
Adv. Mater. 2011, 23, 3061–3065

## Slide 27
H-plasma etching
Adv. Mater. 2011, 23, 3061–3065
L=500 nm, room temp., vacuum
10 mV
Max.
dashed: bulk graphene
500 kΩ
Capac.?

## Slide 28
Edge lithography
Atomic Layer Deposition: selective, prefers edges (dangling bonds, passivated chemical groups)
Nano Lett. 2012, 12, 4642−4646
monolayer GNR

## Slide 29
Edge lithography
Nano Lett. 2012, 12, 4642−4646
top-gated devices:
S, D electrodes defined before ALD (4 nm Al2O3)
10 nm x 700 nm
VDS=1V
vacuum, room temp.
Mobility estimated by them: ~400 cm2/Vs
Mob. estimated by me, supposing a simple model: 840
Mob. est. by me, capac. model of Avouris: 26 cm2/Vs
original graphene edge: mechanically cleaved

## Slide 30
Science 319, 1229 (2008)
Few-layer ribbons
All scale bars 100 nm
Graphite: chemical intercalation of oxidizing sulfuric acid and nitric acid: oxidation of carbon atoms likely occurring at the edge, step, and defect sites
rapid heating of the expandable graphite to 1000°C caused violent formation of volatile gaseous species from the intercalant and exfoliates graphite; thermally desorbing covalently attached species and repair defects
1,2-dichloroethane (DCE) solution of poly(m-phenylenevinylene-co-2,5-dioctoxy-p-phenylenevinylene) (PmPV) by sonication for 30 min; then centrifugation to remove larger pieces: noncovalent functionalization
Deposition+400°C to remove PmPV

## Slide 31
Chemically Derived, Ultrasmooth Graphene Nanoribbons
Science 319, 1229 (2008)
Bilayer, 9 nm x 130 nm
1MΩ
Linear charact. far from the Dirac point
Room temp.
bilayer, 5 nm x 210 nm
Mobility<10?
Their mob. estimation:
100-200

## Slide 32
Chemically Derived, Ultrasmooth Graphene Nanoribbons
Science 319, 1229 (2008)
VDS=0,5V
the off current is thermally activated through a body Schottky-barrier (~Eg) to the cond.band (the barrier for holes is small, like SWNT FETs, because of the high work function of the Pd contacts)
empirical fit: Eg=0,8[eV]/W[nm]
armchair GNR calc.
zigzag GNR calc.
Phys. Rev. Lett. 2008 , 100 , 206803 .

## Slide 33
Unzipping carbon nanotubes
Nature 458, 872-876 (16 April 2009)
solution-based oxidative process for producing a nearly 100% yield of nanoribbon structures by lengthwise cutting and unravelling of multiwalled carbon nanotube (MWCNT) side walls.
Single layer on Si

## Slide 34
as-prepared
N2H4-reduced: 0,03 e2/h
H2-annealed: 0,28 e2/h
300nm wide, 10nm thick (AFM) with a channel length of 500nm
Unzipping carbon nanotubes
Nature 458, 872-876 (16 April 2009)
Reduced and annealed bilayer: Gmin~0,0023 e2/h

## Slide 35
unzipping MWCNTs by plasma etching of nanotubes partly embedded in a polymer film. The GNRs have smooth edges and a narrow width distribution (10–20 nm)
180°
100 nm
Nature 458, 877-880 (16 April 2009)

## Slide 36
Nature 458, 877-880 (16 April 2009)
Unzipping carbon nanotubes
G-band map
Single-layer
16 nm wide, ~200 nm long ribbon after current annealing; in vacuum:
7 nm wide ribbon, in air:
Gmin~0,17 e2/h
Gmin~0,01e2/h
Mob. 20

## Slide 37
Nature Nanotechnology 5, 321 - 325 (2010)
Unzipping „mildly gas-phase oxidized multiwalled carbon nanotubes” using mechanical sonication in an organic solvent; the yield of GNRs is ~2%
TEM:
Almost atomically smoooth edges

## Slide 38
Nature Nanotechnology 5, 321 - 325 (2010)
Unzipping carbon nanotubes
Low ratios of disorder to graphitic Raman bands
~20 nm wide bilayer ribbon

## Slide 39
Fabry-Pérot-like interference pattern at 4,2 K
Nature Nanotechnology 5, 321 - 325 (2010)
Unzipping carbon nanotubes
Random contacts (previous lithography)
1,500 cm2/Vs mobility for 14 nm wide ribbons!
14 nm wide bilayer ribbon, Vb=1mV
Bilayer ribbons with different methods at ROOM TEMP.

## Slide 40
APPLIED PHYSICS LETTERS 94, 082107 2009
QHE at 4K, bulk mobility 7000
Mob. 1250 @ 4K

## Slide 41
method | W (nm) | L (nm) | G min (µS) | G max (µS) | T (K) | µ (cm2/Vs) | source | mob. est. by: | 
EBL+RIE | 24 | 2000 | <0.01 | >4 | 1.7 | 110 | PRL 98, 206805 | ET | 
 | 49 | 2000 | 0.01 | >20 | 1.7 | 215 |  | ET | 
 | 71 | 2000 | 0.5 | >40 | 1.7 | 875 |  | ET | 
 | 85 | 500 | <<1 | >40 | ? | 160-570 | PRL 104, 056801 (2010) | ET | 
 | 30 | 850 | 3 | >14 | 80 | 200 | Avouris PRB 78, 161409 | ET | 
 | 30 | 900 | 1 | >9 | 90 | 165 |  | ET | 
 | 30 | 1700 | <0.1 | >2.5 | 33 | 130 |  | ET | 
 | 100 | 1000 | 11 | >60 | 4 | 530 | Physica E 40 (2007) 228 | ET | 
 | 30 | 200 | <0.15 | >15 | 4.2 | 42 | 0909.3886v2 | ET | 
H-plasma | 6 | 500 | 1.8 | >4 | RT | 18 | Adv. Mater. 2011, 23, 3061 | ET | their mobility estimate >1000
 | 10 | 500 | 3.5 | >10 | RT | 41 |  | ET | 
 | 22 | 500 | 11 | >35 | RT | 51 |  | ET | 
 | 45 | 500 | 35 | >140 | RT | 300 |  | ET | 
 | 80 | 500 | 110 | >300 | RT | 640 |  | ET | 
 | 1000 | 500 | 1200 | >4000 | RT | 3290 |  | ET | 
edge litho | 10 | 700 | 1.5 | >7 | RT | 26 or 400 | Nano Lett. 2012, 12, 4642 | ET/them | 
sonochem. | 9 | 130 | <0.01 | >2 | RT | <10 or 100-200 | Science 319, 1229 (2008) | ET/them | 
AFM LAO | 55 | 800 | 2 | >90 | 4.2 | 1250 | APL 94, 082107 2009 | ET | 
CNT unzip | 14 | 200 | <4 | >116 | 20 | 271 or 1500 | Nature Nano5, 321 (2010) | ET/finite element modelling | 
our GNRs |  |  |  |  |  |  |  |  | 
EBL+plasma | 60 | 570 | <50 | >97 | RT | 17 | 120813cb | my est.based on: | 
 | 60 | 570 | <0.01 | >38 | 4 | 35-188 |  | Avouris PRB 78, 161409 | 
 | 105 | 550 | 10 | >170 | 4 | 990 | 120814cb 1-11 |  | 
 | 80 | 550 | 0.2 | >58 | 4 | 530-765 | 2-9 |  | 
 | 80 | 550 | 2 | >58 | 4 | 660-1200 | 4-8 |  | 
 | 415 | 275 | <54 | >70 | 4 | 22 | 120320ca strip |  | 
 | 110 | 400 | 0 | >15 | 4 | 25 | 121218cp2b 3-4 |  | 
 | 120 | 400 | <0.04 | 4 | 4 | 28-37 | 16-17 |  | 
 | 130 | 400 | 0 | 3 | 4 | 7 | 12-13 |  | 
AFML |  |  |  |  |  |  |  |  | 
120319cd | 30 | 920 | <54 | >116 | RT | 5133 |  |  | 
 | 30 | 920 | <0.01 | <35 | 4 | - |  |  | 
CTE |  |  |  |  |  |  |  |  | 
120320ca | 35 | 70 | ? | <2.1 | 4 | - |  |  | 

## Slide 42
Thank you for your attention!

## Slide 43
Nature Physics 7, 616–620 (2011)
Spatially resolving edge states of
GNRs from unzipping CNTs
7K
atomic order
24 meV
predicted edge state bandgaps

## Slide 44
Nature Physics 7, 616–620 (2011)
Spatially resolving edge states of
GNRs from unzipping CNTs
20 nm wide GNR on Au(111)

## Slide 45
Engineering the edge termination
ACS Nano, 2013, 7 (1), pp 198–202
hydrogen plasma etches away the original edge groups and develops segments with different chiralities along the edge
GNRs from unzipping CNTs, then H-plasma treatment
calc.
room temp.