## Slide 1
Low-temperature STM and transport studies on superconductor-graphene junctions
Zoltán OSVÁTH
Institute of Technical Physics and Materials Science (MFA)
Research Centre for Natural Sciences,
Hungarian Academy of Sciences (MTA TTK)
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 2
1. Low-temperature STM investigation of contacted exfoliated graphene
Zoltán Osváth, Claude Chapelier, and François Lefloch
CEA Grenoble, Institute for Nanoscience and Cryogenics (INAC)
(2008 – 2010)
2. Electric transport measurements on
superconductor-graphene-superconductor (SGS) junctions
Zoltán Osváth, Adrien Allain, Zheng Han, and Vincent Bouchiat
CNRS / NÉEL Institute, Grenoble
(2010 – 2012)
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 3
1. Low-temperature STM investigation of contacted exfoliated graphene
Zoltán Osváth, Claude Chapelier, and François Lefloch
CEA Grenoble, Institute for Nanoscience and Cryogenics (INAC)
Superconducting proximity effect:
L ~ ξT (thermal coherence length)
Goal: study superconducting proximity effect in graphene

## Slide 4
gr
SiO2
e-beam lithography
Ti/Nb/Au (5/40/10 nm) is deposited in a last lithographic step (PTA)
(PMMA 4%, D = 260 µC/cm2, I = 50 pA )
Ti/Nb/Au
Goal: study superconducting proximity effect in graphene
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 5
dI/dV map at EF
0
50
nS
double layer e-beam lithography to improve the metal edge profile:
two PMMA-s with different sensitivities
> 350-400 nm of undercut, smooth edge profile
no ultrasounds for lift-off
AFM image @ RT
(15x15 µm2)
STM image @ 1.6 K
Ti/
Nb/
Au
PMMA 2%
PMMA 4%
lift-off :
STM image (RT)
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 6
690x360 nm2
0
50
nS
dI/dV map at EF :
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 7
Vg (V)
Vbias (mV)
Back-gate voltage dependence of the spectra:
Spectra at a fixed distance (~150 nm ) from the contact
S. Jung, et al., Nature Phys. 7 (2011) 245
EC = e2/Ctot = eΔVbias , EC = 3.4 – 11 meV
Cg = Ctot ∙ (ΔVbias/ ΔVg)
Cg = εA/d, d ≈ 300 nm
D = 30 – 54 nm
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 8
350×210 nm2
85x85 nm2 (Vbias = -1 V, I = 500 pA)
50×32 nm2
Large extrinsic rippling near the contact creates suspended areas:
STM @ 1.5 K
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 9
18×12 nm2
8.5×6.5 nm2
4.5×4.5 nm2
STM @ 1.5 K
Intrinsic rippling on the suspended areas:
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 10
STM/STS at the scale of an extrinsic ripple
dI/dV maps at Vb = 0 mV
(T = 1.6 K)
1 (two hours)
2 (two hours)
3 (two hours)
6.8
13.6
nS
0.5
-0.4
nm
Topography
(32x32 nm2)
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 11
- a disordered 2D system of localized, interacting electrons in thermal equilibrium
there is a continuous rearrangement of the electronic configurations
several pseudo ground states (low energy states)
- the system drifts from one pseudo ground state to another, giving rise to the large fluctuations.
Two-dimensional Coulomb glass:
D. Menashe, O. Biham, B.D. Laikhtman, A.L. Efros, Phys. Rev. B 64 (2001) 115209
x
32x32 nm2
J. Moser, et al., Phys. Rev. B 81 (2010) 205445
(disordered graphene exposed to ozone)
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 12
350×210 nm2
dI/dV(V) spectra:
Vb = − 0.2 V, I = 2 nA, VG = - 25 V
STS at high energy:
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 13
*
*
*
*
*
*
*
*
*
0
1
2
4
6.5×6.5 nm2
STS at high energy on an intrinsic ripple:
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 14
0
1
2
4
6.5×6.5 nm2
Vg (V)
Vbias (V)
STS at high energy on an intrinsic ripple:
Spectra in a fixed position
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 15
0
1
2
4
6.5×6.5 nm2
STS at high energy on an intrinsic ripple
Vg (V)
Vbias (V)
Spectra in a fixed position
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 16
0
1
2
4
6.5×6.5 nm2
STM tip
Variation of C1 :
STS at high energy on an intrinsic ripple:
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 17
STM tip
C1
Cg
Vg
Vb
Si++
SiO2
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 18
Vg (V)
Vbias (V)
EC = 91 meV,
C1 : C2 : Cg = 1045 : 421: 1
 DQD = 3.6 nm
Variation of Vg :
STS at high energy on an intrinsic ripple:
Spectra in a fixed position
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 19
F. Guinea, et al., Phys. Rev. B 77, 075422 (2008)
V. M. Pereira and A. H. Castro Neto,
Phys. Rev. Lett. 103, 046801 (2009)
- local strain induced confinement:
- intrinsic rippling:
J. C. Meyer, et al., Nature 446, 60 (2007)
- strain induced pseudo-magnetic fields
and energy gaps:

## Slide 20
R. Dombrowski, Chr. Steinebach, Chr. Wittneven, M. Morgenstern, and R. Wiesendanger,
Tip-induced band bending by scanning tunneling spectroscopy of the states of the tip-induced quantum dot on InAs(110)
PHYSICAL REVIEW B 59 (1999) 8043

## Slide 21
STS at high energy on an intrinsic ripple:
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 22
182 mV
125 mV
132 mV
139 mV
146 mV
155 mV
165 mV
The peak is measured at the same bias voltage
along constant charge density contours.
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 23
Summary:
- intrinsic rippling of graphene superimposed on the extrinsic rippling induced by the metallic contact.
Low energy spectroscopy on an extrinsic ripple:
observation of a Coulomb gap (suppression of the local DOS at the Fermi level) and slow charge fluctuations  disordered 2D system of localized (), interacting electrons - glass state (T = 1.5 K).
High energy spectroscopy on an intrinsic ripple:
- appearance of a spatially dependent electronic gap and pronounced DOS peaks  formation of graphene quantum dots induced by rippling (T = 1.5 K).
shift of DOS peaks due to the change in the tip-sample capacitance along a ripple.
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 24
2. Electric transport measurements on superconductor-graphene-superconductor (SGS) junctions
Zoltán Osváth, Adrien Allain, Zheng Han, and Vincent Bouchiat
CNRS / NÉEL Institute, Grenoble
Graphene constrictions prepared by O2 plasma etching:
Ti/Pt (10/40 nm)
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 25
AFM
- exfoliated graphene on SiO2
- sharp (crystallografic) edges
Constrictions spontaneously formed during exfoliation:
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 26
exfoliated graphene ribbon (not etched) of ~100 nm in width
contacts: Cr/Pt (5/40 nm)
contacts are larger than designed => incomplete lift-off
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 27
deposition of Pd/Al (5/85 nm),
good resistance (quite transparent contacts): 1.5 kΩ at 50 mK.
Al
Sn
graphene
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 28
T = 50 mK
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 29
E ≈ 0.18 meV
estimation for the phase coherence length:
Lϕ ≈ 11.5 µm at 50 mK
Fabry-Pérot relation:
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 30
Nature 411 (2001) 665
estimation for the
phase coherence length:

## Slide 31
-deposition of Pd/Al/Pd (5/48/7 nm), then Sn (10 nm)
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 32
T=50 mK
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 33
Fabry-Pérot interference:
Distance between interference positions:
ΔVg = 2-5 V, which corresponds to
10-15 mV in Vbias .
- fit with:
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 34
V bias (mV)
1
2
3
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 35
Multiple Andreev reflections:
(highly transparent junction)
1 0.093 mV
2 0.045 mV
3 0.031 mV
4 0.023 mV
5 0.018 mV
6 0.0155 mV
Corrected bias voltages
Vg = 30V
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 36
Temperature dependence (Vg = 30V):
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 37
Corrected
gate map,
showing the
gate dependence
of the dip
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 38
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 39
B = 0 mT
B = 20 mT
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 40
Magnetic field dependence close (Vg = -20V) and far from the Dirac point (Vg = 30V):
Vg = 30 V
Vg = -20 V
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 41
Summary:
fabrication of highly transparent S-G-S junctions using tapered graphene nanostructures (sharp edges).
observation of a Josephson current and multiple Andreev reflections in S-G-S junctions (Andreev billiard).
modulation of both the switching current and normal state resistance by Fabry-Pérot interference  indicates quasi-ballistic transport (T = 50 mK).
estimation for the phase coherence length: Lϕ ≈ 11.5 µm at T = 50 mK.
”ON” and ”OFF” states in the Josephson current: modulated by a gate voltage.
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 42
Acknowledgements:
CEA-Grenoble, INAC
Dr. Marc Sanquer
Dr. Claude Chapelier
Dr. François Lefloch
Dr. Thomas Dubouchet
Dr. Guillaume Albert
Dr. Giorgos Katsaros
CNRS, Institut Néel
Dr. Vincent Bouchiat
Dr. Adrien Allain
Dr. Nedjma Bendiab
Dr. Laetitia Marty
Dr. Valerie Reita
Zheng Han (Vitto)
Thank you for your attention.
Projects: FP7-NMP-2009-SMALL-3 Grenada, the grant Supergraph from the “Agence Nationale de la Recherche”, the French-Hungarian bilateral programme PHC-Balaton/TÉT_10-1-2011-0752, the micro-nano grant Contact metal-graphene from the Rhône-Alpes region, the “Plateforme Technologique Amont de Grenoble”, the project Dispograph financially supported by the “Nanosciences aux limites de la Nanoélectronique” Foundation and the CNRS technology network ReNaTech.

## Slide 46
Vg (V)
Vbias (V)
Vb
VG
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 47
6.5×6.5 nm2
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 49
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 50
AFM Height
AFM Amplitude error
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 51
We can define 3 regions:
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 52
Rwires = 450 Ω
Dip 1: V1 = 0.58 mV; I1 = 0.73 μA; V1’ = V1 – I1×Rwires = 0.25 mV; P1 = I1xV1’ = 0.18 nW
Vg = 30 V
Vg = - 20 V
Dip 1: V1 = 0.58 mV; I1 = 0.52 μA; V1’ = 0.34 mV; P1 = I1xV1’ = 0.18 nW
Dip 2: V1 = 1.05 mV; I2 = 1.25 μA; V2’ = 0.49 mV; P2 = I2xV2’ = 0.61 nW
Dip 3: V1 = 1.41 mV; I3 = 1.66 μA; V3’ = 0.66 mV; P3 = I3xV3’ = 1.1 nW
Dip 2: V1 = 1.1 mV; I2 = 0.96 μA; V2’ = 0.67 mV; P2 = I2xV2’ = 0.64 nW
Dip 3: V1 = 1.4 mV; I3 = 1.21 μA; V3’ = 0.85 mV; P3 = I3xV3’ = 1.03 nW
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 54
STM image (RT)
Problem of PVD:
~ 170 nm high edges, i.e. 3 times higher than the deposited metal (55 nm)
 very difficult to perform low-temperature STM at the metal-graphene interface
PMMA 4%
lift-off : 
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 55
32x32 nm2
1
6.8
13.6
nS
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 56
Vb = -7mV, I = 100 pA, Vg = 25V
-0.4
0.5
nm
8.8
nS
14.8
32x26 nm2
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.

## Slide 57
dI/dV maps at EF
(T = 1.6 K)
32x32 nm2
1
2
3
6.8
13.6
nS
© Copyright 2013. All requests should be sent to: osvath.zoltan@ttk.mta.hu.